| Sample Description | Lab Book Reference | Date |  | Instrument Filename |
| --- | --- | --- | --- | --- |
|  |  | Sample Preparation | FTIR Analysis | FTIR |
| ATR 4-bromostyrene liquid precursor | - | - | 09/04/21 | d513 |
| ATR toluene liquid precursor | - | - | 09/04/21 | d515 |
| RAIRS ASPD 4-bromostyrene / toluene (3:2 v/v) coated silicon substrate | AR485b | 26/02/19 | 09/04/21 | d519 |
| ATR trimethoxyoctylsilane-TiO2 nanoparticles | - | - | 09/04/21 | d516 |
| RAIRS ASPD 4-bromostyrene / toluene + trimethoxyoctylsilane-TiO2 (8% w/v nanoparticle concentration, 3:2 v/v 4-bromostyrene / toluene) coated silicon substrate | AR471b | 01/02/19 | 12/04/21 | d521 |